## Slide 1: Diamond Radiator Development
Brendan Pratt
University of Connecticut
GlueX Collaboration Meeting, Jefferson Lab, February 2012

## Slide 2: Recap from 2011
Excimer Laser refurbished
Translation Stage
Vacuum Chamber Constructed
Optics and Railing Purchased
Chiller (allows for rep rate >3Hz, max 50Hz)
External Triggering circuit designed and built
Data Acquisition Card for pulse measurement
LabView program written
Made our first cuts into Diamond in October 2011

## Slide 3: Results From 2011
Skewed Spot due to Spherical Abberations in Optics

## Slide 4: Old Optics
Single Fused Silica focusing lens creates large spherical aberrations in spot.

## Slide 5: New Optics
L1
L2
L3
First the laser beam is expanded
Setting L1 and L2’s focal lengths at the
Same point
The “Point” is then imaged through
L2, creating a parallel beam
Finally, the light is focused
Through L3, a fused silica lens
With a large radius of curvature (34.5mm)
Onto the target

## Slide 6: Results
This is where I’ll put a picture of a single blast site.

## Slide 7: Using Raster Program
10 steps @
0.05mm increments
14 rows @ 0.05mm increments

## Slide 8
0.7mm
0.9mm
0.5mm

## Slide 9
Trenches show 0.05mm step
After each carriage return

## Slide 10: Vertical Cut

## Slide 11: Single Horizontal Cut
Milling Depth
0.8mm

## Slide 12: Summary
Laser is operating at above ablation energies for hours of run time
Automation of milling cycle is complete
Beam spot has been “cleaned” of spherical aberrations
Will begin milling 20micron diamonds within the next 6 months.

## Slide 13: Questions