## Slide 1: Microscope light guide fiber cladding analysis with SEM/EDX
search for second cladding layer
Richard Jones, Liana Hotte
University of Connecticut

## Slide 2: Overview
SEM - scanning electron microscope
EDX - energy-dispersive X-ray spectroscopy
"EDS - Rimicaris exoculata". Licensed under CC BY 3.0 via Wikimedia Commons

## Slide 3: SEM images - light guide cross sections
old light guide sample
new light guide sample

## Slide 4: SEM images - light guide cross sections
old light guide sample
new light guide sample

## Slide 5: SEM images - light guide cross sections
old light guide sample
new light guide sample

## Slide 6: SEM images - light guide cross sections
old light guide sample
new light guide sample

## Slide 7: EDX images - light guide cross sections
EDX image: old light guide sample
EDX image: new light guide sample

## Slide 8: EDX images - light guide cross sections
EDX image: old light guide sample
EDX image: new light guide sample

## Slide 9: Conclusions
the new lg product clearly has an outer fluorinated layer
it is very thin (5-8 microns vs 40 as claimed in brochure)
thickness seems irregular, maybe missing in places
Take-away message: The new product may be marginally better, but repeating the same construction techniques with the new product is not likely to produce much better results.
A new production method is being tested now